Perpendicular Magnetic tunnel Junctions and
Voltage Controlled Precessional Switching
Meng Xu1, Hamid Almasi1, C. L. Sun2, H. Parraga1, Y. Xu1, X. Li3, T. Newhouse-Illige1, C. Bi1,
P. Khalili Amiri3,4, K. L. Wang3, P.M. Voyles2, and W. G. Wang1
Department of Physics, University of Arizona
2. Department of Materials Science and Engineering, University of Wisconsin
3.Department of Electrical Engineering, UCLA
4. Inston, Inc., Los Angeles
BACKGROUND
Nanosecond reversal of magnetization has been demonstrated in CoFeB/MgO/CoFeB magnetic tunnel junctions with perpendicular anisotropy( pMTJ). Thanks to the voltage controlled magnetic anisotropy (VCMA) effect, nanosecond voltage pulses applied on the pMTJ introduces a temporal change of magnetic easy axis in the free layer, which induces precessional motion of magnetization on the time scale of nanosecond. This mechanism is regarded as a promising way to reduce the switching energy in pMTJs for next generation spintronic memory or logic applications. However, the much appreciated sub-femtojoule energy consumption per bit is still out of reach because of unavoidable joule heating.
I. INTRODUCTION
A. Origin of iPMA at CoFeB/MgO interface
B. pMTJ with W buffer layer
Band specific coefficient (~ 0.2 for Co)
Spin-orbital coupling constant
W could be a good choice of heavy metal layer
in terms of high formation energy with Fe:
Evolution of TMR, GP and GAP reveals less coherent tunneling was
built up in pMTJs compared to MTJs with in-plane anisotropy.
 TAN= 420oC
Annealed 10 min at
Fe-HM	Exp.	Theory
Zr	-	-37 to -13
Nb	-21	-9 to -23
Mo	-4.7 to 3.3	-1 to -3
Ru	-	-7 to -3
Ta	-19	-22 to -9
W	-2.5 to 0.4	0
Hf	-	-30 to -11
Bruno, Phys. Rev. B 39, 865-868 (1989)
Weller et al, Phys. Rev. Lett. 75, 3752-3755 (1995)
out-of-plane/ in-plane orbital moments
Fe
W
Large TMR above 130% was achieved in W/CoFeB/MgO pMTJs
Mg
Compared to Ta-pMTJs, W-pMTJs R drop faster during extended high
temperature annealing.
Fe
W-pMTJ shows larger roughness
W interdiffuses into MgO barrier more easily
B. Voltage controlled magnetic anisotropy
Ta
Mg
Junctions were annealed at 420oC for 3.5h
C. VCMA and switching measurement
Voltage controlled magnetic anisotropy (VCMA)
through charge transfer through different orbitals
and spin-orbit coupling at interface
18 fJ with switching probability of 99% at 400ps
TMR=142%
Nature Nanotechnology 4, 158 - 161 (2009)
C. Voltage induced precession
Switching data measured at from normal
MR curve measured at from normal
D. Field dependent switching measurement
TMR=130%
When a nanosecond scale voltage pulse is applied to sufficiently small MTJ, magnetic
easy axis becomes in plane and Larmor precession is induced through LLG equation.
All pulses are -2V in amplitude,
1ns in duration
Large modulation of switching energy by changing the field angle, 7.7 fJ switching
with 82% probability can be achieved by this method with -1.8V and 500ps pulses
II. FABRICATION AND MEASUREMENT
IV. HIGHLIGHTS
Significantly improved TMR and thermal stability in pMTJ by Mo dusting
Fabricated MTJs with W buffer layer and studied its structural evolution during annealing using TEM
CoFeB/MgO/CoFeB MTJ nanopillar(D=100nm) with high TMR(142%), thermal stability
     over 40 and large voltage effect was fabricated to achieve ultrafast precessional
     switching.
Large modulation of switching energy by tuning static magnetic field.
Magnetron Sputtering
Metallic layers grown by DC sputtering at 2mTorr
MgO barrier grown by RF sputtering at 0.6-1 mTorr
Standard photolithography and nanosphere lithography to fabricate nanopillars with D=100nm
V. NEXT STEPS
III. RESULTS AND DISCUSSION
Reduce switching energy by enhancing VCMA efficiency and reducing damping.
Explore VCMA effect based on voltage controlled Rashba spin-orbit effect, which can be tuned by different under layers.
Further enhance TMR, PMA. Study precessional switching in smaller devices.
A. pMTJ with insertion of Mo-dusting layers
Heat of Formation (kJ/mol)
Ta(8)/CoFeB(5)/MgO
Mo(8)/CoFeB(5)/MgO
Ta(8)/Mo(0.9)/CoFeB(5)/MgO
Fe-HM	Exp.	Theory
Zr	-	-37 to -13
Nb	-21	-9 to -23
Mo	-4.7 to 3.3	-1 to -3
Ru	-	-7 to -3
Ta	-19	-22 to -9
W	-2.5 to 0.4	0
Hf	-	-30 to -11
ACKNOWLEDGMENTS
This work was supported in part by C-SPIN, one of the six centers of STARnet, a Semiconductor Research Corporation program, sponsored by MARCO and DARPA.
Dusting dramatically help with TMR
        Record high TMR (208%) in voltage-controllable pMTJs
        New approach to simultaneously improve TMR, PMA and VCA
Mo has strong 110 texture: bad for CoFeB
Ta is amorphous: but small formation energy
     with Fe
Mo dusting combines advantages of both
Fe
MgO(100)
Hybrid of Fe 3d with O 2pZ at interface
ml(001)>ml(100) via SOC induces PMA
Fe 3d-z2
O 2pz
Niranjan et. al. Appl. Phys. Lett. 96, 222504 (2010)
Shimabukuro et. al. Physica E 42, 1014-1017 (2010)
Yang et. al. Phys. Rev. B 84, 054401(2011)
Ta(6)
Si/SiO2
Ru(8)
Ta(10)
CoFeB(0.85)
MgO(1-3)
CoFeB(1.5)
Ta(10)
Ru(20)
Ta(3)
Si/SiO2
Ru(6)
Ta(4)
CoFeB(0.85)
MgO(1-3)
CoFeB(1.5)
Ta(5)
Ru(14)
Ta(10)
W(6)
Si/SiO2
Ru(8)
W(10)
CoFeB(0.85)
MgO(1-3)
CoFeB(1.5)
W(10)
Ru(20)